## Slide 1
Lecturer: Mitsuaki Kawamura (河村光晶)
物質科学のための計算数理 II
Numerical Analysis for Material Science II
8th: Density Functional Theory (1)
Nov. 30 (Fri)

## Slide 2: Schedule (This semester W1, W2)
Sep. 28 (Fri) Guidance Y
Oct. 5 (Fri) Monte Carlo method O
Oct. 12 (Fri) Monte Carlo method O
Oct. 19 (Fri) Monte Carlo method O
Oct. 26 (Fri) Exact diagonalization Y
Nov. 2 (Fri) Exact diagonalization Y
Nov. 9 (Fri) Molecular dynamics O (1st report problem will be announced.)
Nov. 30 (Fri) Standard DFT code K
Dec. 7 (Fri) Density functional theory K
Dec. 14 (Fri) Density functional theory K
Dec. 21 (Fri) Density functional theory K
Dec. 25 (Tue) (2nd)Report problem K (遠隔講義室)
Jan. 11 (Fri) Density functional theory K
※ Lecturers: Y … Yamaji, K … Kawamura, O… Ohgoe

## Slide 3: Schedule in this section (DFT)
Nov. 30 (Fri) Standard DFT code
  First-principles calculation and Density functional theory (Lecture)
  One-body Schrödinger eq. for periodic system and Bloch theorem (L)
  Numerical solution of Kohn-Sham (one-body Schrödinger) eq. (L)
  Hands-on DFT code (Tutorial)
  Version control system : Git (T)
Dec. 7 (Fri) Kohn-Sham eq.
  Plane-wave basis and Pseudopotentials (L)
  Iterative eigenvalue solution method (L & T)
Dec. 14 (Fri) Self-Consistent loop
  Hartree potential (Poisson eq.)
  Brillouin-zone integral (Tetrahedron method)
  Visualization (T)
Dec. 21 (Fri) Total Energy
  Coulomb potential for periodic point charge (Ewald sum)
Dec. 25 (Tue) (2nd)Report problem K (遠隔講義室)
Jan. 11 (Fri) Density functional theory K

## Slide 4: Today’s Schedule
What is the first-principles study
Density functional theory
Kohn-Sham method
Periodic system (Bulk crystal)
Bloch theorem
How to solve Kohn-Sham eq. with computer
DFT code
Git clone
Charge density
Band structure
Fermi surface
Density of states (DOS), Partial DOS

## Slide 5: Electrons in materials
Information of electronic structure
Charge density
Magnetic moment
Superconductivity
Optical spectrum
etc.
Single H2O molecule : N = 10
Single C60 molecule : N = 360
Bulk crystal, liquid, glass, ・・・ :
N > 1024
Both numerically and analytically unsolvable.
Can we obtain a few quantities such as
Ground-state energy
Ground-state charge density
without solving this equation ?

## Slide 6: Density functional theory
Universal functional exists.
Functional depends on the overall shape of , e.g.,
Hohenberg-Kohn theorem
Phys. Rev. 136, B864 (1964).

## Slide 7: Kohn-Sham method
Kinetic energy of non-interacting system whose charge density is
The exact form of is not known.
Approximate
Self-consistent field (SCF)
W. Kohn and L. J. Sham,
Phys. Rev. 140, A1133 (1965).

## Slide 8: Local density approximation
: Function (not functional)
: Use the XC energy of homogeneous-electron gas
Random phase approximation :
Monte-Carlo method
: Generalized gradient correction (GGA)
M. Gell-Mann and K. A. Brueckner, Phys. Rev. 106, 364 (1957).
[Monte-Carlo] D. M. Ceperley and B.J. Alder, Phys. Rev. Lett. 45, 566 (1980).
[Parameterize] J. P. Perdew and A. Zunger, Phys. Rev. B 23, 5048 (1981).

## Slide 9: Total energy and force
Hellman-Feynmann theorem
Finding the lowest-energy (stable) structure
Structure optimization : One of the most popular usage of DFT
Nuclear-nuclear interaction

## Slide 10: Structure optimization
GGA-PBE functional : J. Perdew, K. Burke, and M. Ernzerhof Phys. Rev. Lett. 77, 3865 (1996)
Other usage : Formation (Cohesive) energy
A + B → C + Energy
Magnetic moment (Spin density functional theory) :

## Slide 11: Kohn-Sham eq. for periodic system (1)
and are periodic,
i.e.,
Equation to solve in the whole region of bulk crystal
Unit lattice vectors (Not unique)
electrons per unit cell
cells → ∞
Unit cell

## Slide 12: Kohn-Sham eq. for periodic system (2)
Equation to solve only in the unit cell
Unit reciprocal lattice vectors
can be written as
Bloch’s theorem
and is
periodic with in the space.
Band structure

## Slide 13: One-body energy level
True quasi-particle energy
Qualitative analyzation
Angle resolved photo electronic spectroscopy
de Haas-van Alphen oscillation
e
e
e
e
Inversed magnetic field (1/H)
Susceptibility
X. Zhu and S. Louie, Phys. Rev. B 43, 14142 (1991).
Unit [eV] | LDA | GW | Exp.
Si | 0.54 | 1.32 | 1.17
LiCl | 6.07 | 9.34 | 9.40
AlP | 1.52 | 2.59 | 2.50
AlAs | 1.25 | 2.15 | 2.23
AlSb | 0.99 | 1.64 | 1.68
GaP | 1.82 | 2.55 | 2.39
GaAs | 0.37 | 1.22 | 1.52
InP | 0.57 | 1.44 | 1.42
Band gap

## Slide 14: How to solve Kohn-Sham eq. : Basis
→
Huge numerical cost !
Not efficient.
Pseudopotential (plane wave, real space grid, FEM)
Local basis (atomic orbital, Gaussian)
Augmented wave (complicated basis)
Mixed basis (PW + Local, augmented + Local)
Plane waves below the
Cutoff frequency

## Slide 15: Pseudopotential
Electronic state at core level (e.g. 1s state for Fe)
hardly affects the chemical properties
(chemical reaction, conduction, superconductivity, etc.)
Pseudopotential is generated
in the calculation of single atom
only reproduce the
energy and long-range behavior
of valence state.
Similar to the potential of an ion.
Then,
used for the calculation of
molecule, solid, etc.
Transferability
1s
2s
2p
valence
True
Pseudo
Norm conserving
Ultrasoft
Projector augmented wave

## Slide 16: QuantumESPRESSO: plane wave and pseudopotential based code
Before the explanation, we should start to install because it takes long time.
$ mkdir -p ~/bin/
$ echo 'export PATH=$HOME/bin:$PATH' >> ~/.profile
$ git clone https://gitlab.com/QEF/q-e.git -b qe-6.3 ~/q-e
$ cd ~/q-e/
$ ./configure CC=gcc-8; make pw pp; cp bin/* ~/bin/
mac OSX in ECCS
Prompt. We do not need type this.

## Slide 17: Quantum ESPRESSO
Web page : https://www.quantum-espresso.org/
Developer : P Giannozzi (University of Udine, Italy), et al. (Many)
Language : Fortran (Mainly)
Feature:
  Total energy, force, MD, chemical reaction path, charge/spin density
  Band structure, density of states, Fermi surfaces
  LDA, GGA, Van der Waals, exact exchange functional
  MPI+OpenMP parallelism, GPGPU
  Phonon and electron-phonon interaction
  X-ray absorption spectra, Optical spectra
  Many-body perturbation theory (GW, Bethe-Salpeter eq.)
  Wannier function, Berry's phase
  Etc.
Manuals : https://www.quantum-espresso.org/resources/users-manual
Pseudopotential library
  SSSP (https://www.materialscloud.org/discover/sssp/table/efficiency)
  PSLibrary (https://www.quantum-espresso.org/pseudopotentials)

## Slide 18: Visualization tools
$ git clone https://scm.osdn.net/gitroot/fermisurfer/fermisurfer.git -b 1.10.1 ~/fermisurfer
$ cd ~/fermisurfer/
$ touch Makefile.in aclocal.m4 configure
$ ./configure --prefix=$HOME; make; make install
FermiSurfer : Fermi-surface viewer
VESTA : Crystal-structure viewer (Also charge density, etc.)
$ wget https://jp-minerals.org/vesta/archives/3.4.5/VESTA.dmg
$ hdiutil mount VESTA.dmg
$ cp -rf /Volumes/VESTA/VESTA ~/
$ echo 'alias vesta="open -a $HOME/VESTA/VESTA.app"' >> ~/.profile
$ source ~/.profile

## Slide 19: Tutorial : MgB2
$ wget https://osdn.net/projects/educational-pwdft/storage/113018.tgz
$ tar xzvf 113018.tgz -C ~/
$ cd ~/113018/
$ vesta mgb2.xsf
Metal
Superconductivity : TC = 39 K
Stacked Mg triangular lattice and B honeycomb lattice

## Slide 20: Structure optimization & input file
$ mpirun -np 2 ~/bin/pw.x -npool 2 -in relax.in | tee relax.out
&CONTROL
calculation = 'vc-relax'
pseudo_dir = './'
/
&SYSTEM
ibrav = 0
nat = 3
ntyp = 2
ecutwfc = 35.000000
ecutrho = 280.000000
occupations = 'tetrahedra_opt'
/
&ELECTRONS
/
&IONS
/
&CELL
/
Variation-cell structure relaxation
Number of atoms in the unit cell
Number of kinds of atom
Cutoff energy of plane-waves for
wave functions [Ry]
Cutoff energy of plane-waves for
the charge density [Ry]
Integration scheme for the
numerical integration in
Cutoff depends on the pseudopotential

## Slide 21: Input-file format
CELL_PARAMETERS angstrom
3.200000 0.000000 0.000000
-1.600000 2.771281 0.000000
0.000000 0.000000 3.700000
ATOMIC_SPECIES
B 10.811000 b_pbe_v1.4.uspp.F.UPF
Mg 24.305000 Mg.pbe-n-kjpaw_psl.0.3.0.UPF
ATOMIC_POSITIONS crystal
Mg 0.000000 0.000000 0.000000
B 0.333333 0.666667 0.500000
B 0.666667 0.333333 0.500000
K_POINTS automatic
12 12 8 0 0 0
Unit lattice vectors (Å unit)
Element
Relative atomic mass
Pseudopotential file name
-mesh for numerical integration in
Atomic position in the
fractional coordinate
Dense k-mesh improves accuracy and increases numerical cost.

## Slide 22: Result
$ grep volume relax.out
relax.out: unit-cell volume = 221.4261 (a.u.)^3
relax.out: new unit-cell volume = 204.22304 a.u.^3 ( 30.26273 Ang^3 )
relax.out: new unit-cell volume = 193.53924 a.u.^3 ( 28.67956 Ang^3 )
relax.out: new unit-cell volume = 194.50016 a.u.^3 ( 28.82195 Ang^3 )
relax.out: new unit-cell volume = 194.38563 a.u.^3 ( 28.80498 Ang^3 )
relax.out: new unit-cell volume = 194.25661 a.u.^3 ( 28.78586 Ang^3 )
relax.out: new unit-cell volume = 194.25661 a.u.^3 ( 28.78586 Ang^3 )
relax.out: unit-cell volume = 194.2566 (a.u.)^3
$ grep -A 3 CELL_PARAMETERS relax.out
CELL_PARAMETERS (angstrom)
3.106677678 0.000000000 -0.000000000
-1.553338839 2.690461490 0.000000000
0.000000000 -0.000000000 3.620638395
:
--
CELL_PARAMETERS (angstrom)
3.072422829 0.000000000 0.000000000
-1.536211414 2.660795917 0.000000000
0.000000000 0.000000000 3.521167214
Exp. (XRD)
a = 3.085 Å, c = 3.523 Å
volume : 29.04 Å3

## Slide 23: Band structure
$ mpirun -np 2 ~/bin/pw.x -npool 2 -in nonscf.in
$ mpirun -np 2 ~/bin/bands.x -npool 2 -in bands.in
$ gnuplot band.gp
$ mpirun -np 1 ~/bin/pp.x -npool 1 -in pp.in
$ vesta tmp.pp_K001_B00*.xsf
Γ
M
K
A
L
H

## Slide 24: Density of states & Fermi surface
$ mpirun -np 2 ~/bin/pw.x -npool 2 -in dense.in
$ mpirun -np 2 ~/bin/projwfc.x -npool 2 -in pdos.in |tee pdos.out
$ gnuplot pdos.gp
$ mpirun -np 1 ~/bin/fermi_proj.x -in proj_pz.in
$ mv proj.frmsf pz.frmsf
$ mpirun -np 1 ~/bin/fermi_proj.x -in proj_pxy.in
$ mv proj.frmsf pxy.frmsf
$ fermisurfer pz.frmsf
$ fermisurfer pxy.frmsf
Fermi surface :
Isosurface at

## Slide 25: Why do we perform DFT calculation ?
Force or total energy.
Directly compute (predict)
properties of materials.
Fit into model atomic force field.
Perform classical MD for
large-size system or log-time scale.
Compute effective single-body state,
Kohn-Sham orbitals.
Construct Hubbard model or local spin model.
Perform Monte-Carlo simulation, exact diagonalization for more accurate calculation of exotic phenomena.
DFT calculation

## Slide 26: Today's summary
Basics of DFT calculation
  Hohenberg-Kohn theorem
  Kohn-Sham method
  Exchange correlation functional
  Total energy and force
Kohn-Sham eq. in periodic system (bulk crystal)
  Bloch theorem
  Band structure
Numerical method to solve Kohn-Sham eq.
  Plane-wave (and other) basis
  Pseudopotential
Usage of a DFT code : Quantum ESPRESSO

## Slide 27: Reference books
Electronic Structure: Basic Theory and Practical Methods
Richard M. Martin
Cambridge University Press
Errata : https://es.polytechnique.fr/Electronic_Structure/errata
日本語訳
物質の電子状態 上下
寺倉清之、寺倉郁子、善甫康成
シュプリンガー
固体‐構造と物性
金森 順次郎, 川村 清, 米沢 富美子, 寺倉 清之
岩波
絶版
岩波オンデマンド