## Slide 1
Lecturer: Mitsuaki Kawamura (河村光晶)
物質科学のための計算数理 II
Numerical Analysis for Material Science II
9th: Density Functional Theory (2)
Dec. 7 (Fri)

## Slide 2: Schedule (This semester W1, W2)
Sep. 28 (Fri) Guidance Y
Oct. 5 (Fri) Monte Carlo method O
Oct. 12 (Fri) Monte Carlo method O
Oct. 19 (Fri) Monte Carlo method O
Oct. 26 (Fri) Exact diagonalization Y
Nov. 2 (Fri) Exact diagonalization Y
Nov. 9 (Fri) Molecular dynamics O (1st report problem will be announced.)
Nov. 30 (Fri) Standard DFT code K
Dec. 7 (Fri) Density functional theory K
Dec. 14 (Fri) Density functional theory K
Dec. 21 (Fri) Density functional theory K
Dec. 25 (Tue) (2nd)Report problem K (遠隔講義室)
Jan. 11 (Fri) Density functional theory K
※ Lecturers: Y … Yamaji, K … Kawamura, O… Ohgoe

## Slide 3: Schedule in this section (DFT)
Nov. 30 (Fri) Standard DFT code
  First-principles calculation and Density functional theory (Lecture)
  One-body Schrödinger eq. for periodic system and Bloch theorem (L)
  Numerical solution of Kohn-Sham (one-body Schrödinger) eq. (L)
  Hands-on DFT code (Tutorial)
  Version control system : Git (T)
Dec. 7 (Fri) Kohn-Sham eq.
  Plane-wave basis and Pseudopotentials (L)
  Iterative eigenvalue solution method (L & T)
Dec. 14 (Fri) Self-Consistent loop
  Hartree potential (Poisson eq.)
  Brillouin-zone integral (Tetrahedron method)
  Visualization (T)
Dec. 21 (Fri) Total Energy
  Coulomb potential for periodic point charge (Ewald sum)
Dec. 25 (Tue) (2nd)Report problem K (遠隔講義室)
Jan. 11 (Fri) Density functional theory K

## Slide 4: Today’s Schedule
Kohn-Sham eq. in periodic system
Plane-wave representation
Iterative diagonalization
Matrix-vector product
Kinetic energy term
Potential term
Visualize

## Slide 5: Kohn-Sham method
Kinetic energy of non-interacting system whose charge density is
Self-consistent field (SCF)
last week

## Slide 6: Kohn-Sham eq. for periodic system (1)
is periodic,
i.e.,
Equation to solve in the whole region of bulk crystal
Unit lattice vectors (Not unique)
electrons per unit cell
cells → ∞
Unit cell
last week

## Slide 7: Kohn-Sham eq. for periodic system (2)
Equation to solve only in the unit cell
Unit reciprocal lattice vectors
can be written as
Bloch’s theorem
and is
periodic with in the k space.
Band structure
last week

## Slide 8: How to solve Kohn-Sham eq. : Basis
last week

## Slide 9: Unit in this lecture
Inside program code:
Length : Atomic unit (Bohr radius). 1 [Bohr] = 0.529177249 [Å]
Energy : Atomic unit (Hartree). 1 [Eh] = 27.21138456 [eV]
Input and output :
Length : Angstrom
Energy : Electron volt
Useful to read by VESTA
[Bohr-1]
[Eh]
[Eh]

## Slide 10: Fourier Transformation
Discretize (considering one dimension)
→ ∞ : Exact
numerical cost
Fast Fourier Transformation (FFT) : numerical cost
We do not detail in this lecture. We just use FFT numerical library.

## Slide 11: Cutoff frequency

## Slide 12: Very simple plane-wave DFT program
$ cd ~
$ git clone git://git.osdn.net/gitroot/educational-pwdft/pwdft.git
$ cd pwdft
$ cp make.inc.mac make.inc
$ make
$ cd sample/Al/
$ ../../src/pwdft.x < direct.in
Aluminum
Face centered cubic (fcc)
Metal
Almost free electron
keep
"ecutrho" ≧ 4*ecutwfc
&CONTROL
calculation = 'direct'
/
&SYSTEM
nbnd = 10
nat = 1
ntyp = 1
ecutwfc = 60.000000
ecutrho = 240.000000
/
&ELECTRONS
/
CELL_PARAMETERS
0.000000 2.024700 2.024700
2.024700 0.000000 2.024700
2.024700 2.024700 0.000000
ATOMIC_SPECIES
Al al.lda.lps
ATOMIC_POSITIONS
Al 0.000000 0.000000 0.000000
K_POINTS
1
0.0 0.0 0.0
Only perform first SCF step
Initial density is
uniform

## Slide 13: direct@diag_direct.F90
lwork = -1
allocate(work(1))
call zheev('V', 'U', npw, ham, npw, eval_full, work, lwork, rwork, info)
lwork = nint(dble(work(1)))
deallocate(work)
allocate(work(lwork))
call zheev('V', 'U', npw, ham, npw, eval_full, work, lwork, rwork, info)
deallocate(work)
Workspace (memory size) query : Do not need to care.
Diagonalize Hamiltonian matrix "ham"
Computational cost :
Memory size :
Changing "ecutrho" and "ecutwfc"
and see "Kohn-Sham Time" in Standard output
keep ecutrho ≧ 4*ecutwfc
Large numerical cost for large
We only need lower energy (occupied) band.
http://mitsuaki1987.github.io/pwdft/index.html

## Slide 14: Locally Optimal Block Preconditioned Conjugate Gradient (LOBPCG) method
One of the iterative eigen solution methods
A. V. Knyazev, SIAM J. Sci. Compute. 23, 517 (2001).
山田進 他, 日本計算工学会論文集, 20060027 (2006).
For computing eigenvector, at each step
Approx. eigenvector
Residual vector
CG vector
Construct subspace Hamiltonian ( dim.)
Diagonalize with direct method
Take lowest vectors as approximate eigenvectors at next step
Loop until all become smaller than the threshold
Computational cost :
Memory :

## Slide 15: Algorithm of LOBPCG method lobpcg_main@lobpcg.F90
Initial guess (Random or atomic)
do iteration
All are small enough ? → Exit
Solve
Take lowest :
end do iteration

## Slide 16: Hamiltonian vector product h_psi@hamiltonian.F90
Done in subroutine hpsi in hamiltonian.F90

## Slide 17: Running iterative method
$ cd ~/pwdft/sample/Al/
$ ../../src/pwdft.x < iterative.in
&CONTROL
calculation = 'iterative'
/
&SYSTEM
nbnd = 10
nat = 1
ntyp = 1
ecutwfc = 60.000000
ecutrho = 240.000000
/
&ELECTRONS
/
CELL_PARAMETERS
0.000000 2.024700 2.024700
2.024700 0.000000 2.024700
2.024700 2.024700 0.000000
ATOMIC_SPECIES
Al al.lda.lps
ATOMIC_POSITIONS
Al 0.000000 0.000000 0.000000
K_POINTS
1
0.0 0.0 0.0
See "Kohn-Sham Time" in
Standard output
keep ecutrho ≧ 4*ecutwfc

## Slide 18: Report problem 1
(1) Compare the computational time of direct method and LOBPCG method by changing ecutrho and ecutwfc.
keep ecutrho ≧ 4*ecutwfc
ecutwfc [Ry]
Time [sec]
(2) Plot the cutoff-energy dependence of Kohn-Sham energy for
and (they are outputted to a file band.dat).

## Slide 19: What is the command "git"
$ git clone ssh://user-name@133.11.72.58:/home/Student/Public/pwdft
Backup code
Port program in any system
Merge modifications
Compare diff
Log each modification with comment
Etc.

## Slide 20: Considered case 1
Laptop PC
Labo PC
Home PC
PC cluster
System C
System B
・ Where is the latest source code ?
・ We need to update source code easily.

## Slide 21: Considered case 2
Program
Program
Program
Program
Speed up with symmetry
OpenMP
OpenMP+MPI
System A
System B
System A
System A
System A
System B
・ We need to trace when was it broken.
・ We need to be available to return the stable (no error) code.

## Slide 22: Version control
Repository
server
Program (commit 1)
Program (commit 2)
Program (commit 3)
Program (commit 10)
$ git pull
Update latest version
Latest
local repository
Modify
Program (commit 11)
$ git commit
$ git push
local repository
$ git pull
update modification
Logging :
Who
When
What
modified

## Slide 23: When modified simultaneously
Repository
server
Program (commit 1)
Program (commit 2)
Program(commit 3)
Program (commit 10)
Latest
local repo
commit
Program (commit 11)
local repo
commit 10+
$ git push
Program (commit 12)
$ git pull
commit 11+
$ git push

## Slide 24: Tutorial
$ cd ~/pwdft/
$ git branch -a
$ git config --global user.name "user-name"
$ git config --global user.email "user-name@bkks"
$ git checkout -b user-name
$ echo "Hello, I am user-name." > user-name.txt
$ git add user-name.txt
$ git commit (vi is used)
$ git push --set-upstream origin user-name
$ git branch -a

## Slide 25: Example of branches
Master
Develop
Feature (new features)
Hotfix (Bug fix)
Release
V0.1
V0.2
V1.0
"A successful branch in git"

## Slide 26: Today's summary
Plane-wave representation of Kohn-Sham eq.
Direct method and LOBPCG method
Hamiltonian-vector product with FFT
Git